Rice husk ash waste as effective reinforcement in the polymer matrix composites/nanocomposites for electronic applications

V. S. Darekar, R. D. Gadve and R. K. Goyal

Department of Metallurgical and Materials Engineering, Malaviya National Institute of Technology Jaipur, Jaipur-302017, India

Email: rkg.meta@mnit.ac.in

Agricultural wastes are finding importance in the polymer industry due to their light weight, low cost and being environmentally friendly. Current study discusses the use of rice husk ash (RHA) obtained after pyrolysis at a temperature of about 550 °C for the electronic applications such as printed circuit boards (PCBs), electronic substrates, radar absorbing materials (RAMs) etc. Amorphous RHA containing more than 94 wt.% SiO2 with remaining amounts of other oxides were synthesized and ball milled to reduce its particle size. The resultant powder was used as a reinforcement (0-30 wt.%) in the polymer matrices. The thermal, electrical, and mechanical properties of the resultant composites/nanocomposites were investigated. Scanning electron microscopy revealed uniform dispersion of RHA in the polymer matrix and good interfacial adhesion between them. The addition of RHA particles increased the char yield, dimensional stability, thermal conductivity and dielectric properties which indicated that the composites have potential applications for the PCBs. Moreover, the addition of RHA synthesized under the controlled atmosphere were found a good reinforcement in enhancing microwave absorbing properties (in the X-band) as well as mechanical properties, thus, making resultant composites as potential candidates for the radar absorbing materials applications.

References:

- V. S. Darekar, M. G. Kulthe, A. Goyal, R. K. Goyal, J. Electron. Mater. 53, 2024, 1344.

- R. D. Gadve, Y. Trivedi, V. K. Sangal, V. M. Sreekumar, R. K. Goyal, J. Mater. Sci.: Mater. Electron 34, 2023, 1953.

- M. Joshi, R. Gadve, G. Upadhyay, R. K. Goyal, J. Mater. Sci.: Mater. Electron. 34, 2023, 2276.